## Slide 1: Howie Moseley State Bituminous Materials Engineer
Florida Department of
TRANSPORTATION
State of the Industry

## Slide 2: My Contact Information

## Slide 3: State Highway System
44,975 lane miles
  8,677 interstate lane miles (19%)
  33,937 arterial lane miles (76%)
  2,361 Turnpike lane miles (5%)
97.3% of pavement is asphalt
2.7% of pavement is concrete

## Slide 4: Asphalt Surfaces
50.4% of asphalt surfaces are dense graded (by lane mile)
49.6% of asphalt surfaces are open graded

## Slide 5: Asphalt Producers for Florida
 | In-State | Out-of-State
Asphalt Plants | 97 | 2
Asphalt Contractors | 38 | 2
Asphalt Binder Terminals | 15 | 10
Asphalt Emulsion Terminals | 5 | 8

## Slide 6: Approved Asphalt Plants

## Slide 7: Approved Asphalt Binder Terminals

## Slide 8: Approved Asphalt Emulsion Terminals

## Slide 9: Asphalt Mix Tonnage (FY 19/20)
Friction |  |  | Structural |  |  | Total
FC-5 | FC-12.5 | FC-9.5 | SP-9.5 | SP-12.5 | SP-19.0 | 
505,791 | 460,602 | 146,268 | 91,902 | 3,155,161 | 86,366 | 4,447,880

## Slide 10: Asphalt Tonnage By District (FY 19/20)

## Slide 11: Asphalt Tonnage By Producer (FY 19/20)

## Slide 12: Asphalt Tonnage By Producer (FY 19/20)
Chart: Asphalt Mix Tonnage

## Slide 13: Mix Tonnage By Traffic Level (FY 19/20)

## Slide 14: Friction Course Aggregate Type (FY 19/20)

## Slide 15: Mix Tonnage By Binder Type (FY 19/20)
Total mix tonnage 4,447,880

## Slide 16: Binder Tonnage (FY 19/20)
Total binder tonnage 246,921

## Slide 17: RAP Usage
- 775,000 Tons of RAP
- 50,000 Tons of Binder from RAP
- 725,000 Tons of Aggregate from RAP

## Slide 18: RAP Usage
Condition | FY 11/12 | FY 12/13 | FY 13/14 | FY 14/15 | FY 15/16 | FY 16/17 | FY 17/18 | FY 18/19 | FY 19/20
Unrestricted (no limit) |  |  |  |  |  |  |  |  | 
Average | 26% | 25% | 29% | 24% | 29% | 27% | 24% | 25% | 24%
Maximum | 38% | 39% | 45% | 50% | 50% | 50% | 50% | 50% | 50%
Restricted (Max 20%) |  |  |  |  |  |  |  |  | 
Average | 18% | 16% | 19% | 20% | 20% | 19% | 19% | 19% | 18%
Maximum | 20% | 20% | 20% | 20% | 20% | 20% | 20% | 20% | 20%

## Slide 19: Asphalt Mix Cost

## Slide 20: Asphalt Mix Weighted Average Cost ($/ton)

## Slide 21: Asphalt Binder Cost

## Slide 22: Asphalt Price Index

## Slide 23: 2021 High Polymer Binder Forecast

## Slide 24: Pay Factor Data

## Slide 25: Composite Pay Factor (CPF) Data
Statewide Average CPF
  FY 19/20: 1.018
  FY 18/19: 1.016
  FY 17/18: 1.016
  FY 16/17: 1.013
  FY 15/16: 1.009
  FY 14/15: 1.018
  FY 13/14: 1.019
  FY 12/13: 1.011

## Slide 26: Composite Pay Factor (CPF) Data
Dense Graded Pay Factor Data
FY | Density | AC | Air Voids | #8 Sieve | #200 Sieve | CPF
19/20 | 1.000 | 1.032 | 1.027 | 1.003 | 1.033 | 1.018
18/19 | 0.992 | 1.025 | 1.021 | 1.001 | 1.028 | 1.015
17/18 | 0.999 | 1.032 | 1.023 | 1.002 | 1.027 | 1.016
16/17 | 0.992 | 1.031 | 1.024 | 0.997 | 1.025 | 1.013
15/16 | 0.994 | 1.023 | 1.013 | 1.003 | 1.019 | 1.009
14/15 | 1.004 | 1.029 | 1.024 | 0.998 | 1.031 | 1.018
13/14 | 1.003 | 1.031 | 1.026 | 1.011 | 1.030 | 1.020

## Slide 27: Composite Pay Factor (CPF) Data
Open Graded Pay Factor Data
FY | AC | 3/8” Sieve | #4 Sieve | #8 Sieve | CPF
19/20 | 1.019 | 1.020 | 1.020 | 1.012 | 1.019
18/19 | 1.007 | 1.021 | 1.019 | 1.011 | 1.018
17/18 | 1.012 | 1.017 | 1.013 | 1.013 | 1.014
16/17 | 1.011 | 1.012 | 1.015 | 1.018 | 1.014
15/16 | 1.004 | 1.005 | 1.002 | 1.013 | 1.004
14/15 | 1.019 | 1.021 | 1.018 | 1.026 | 1.019
13/14 | 1.015 | 1.007 | 1.009 | 1.032 | 1.014

## Slide 28: FY 19/20 Top Producer CPF (>100,000 tons)
#1 Preferred Materials (1.0361)
#2 General Asphalt (1.0274)
#3 Halley Engineering (1.0267)

## Slide 29: FY 19/20 Top Producer CPF (25,000-100,000 tons)
#1 Group III (1.0413)
#2 Peavy & Son (1.0394)
#3 Asphalt Group (1.0385)

## Slide 30: Quality Control That Adds Value

## Slide 31: Quality Control That Adds Value

## Slide 32: Quality Control That Adds Value
Bond Strength Testing
Most contractors already have a Marshall test press
Every contractor already cuts cores
The only other equipment that is needed is the interlayer bond strength tester and shims

## Slide 33: Quality Control That Adds Value
Use test results for information purposes
Can help assess the effectiveness of your paving operations and minimize potential warranty issues
FM 5-599: Determining the Interlayer Bond Strength Between Asphalt Pavement Layers
  https://fdotwww.blob.core.windows.net/sitefinity/docs/default-source/materials/administration/resources/library/publications/fstm/methods/fm5-599.pdf?sfvrsn=f8e357fc_4

## Slide 34: Quality Control That Adds Value
End of Load Segregation
You can’t always see it while your paving
But you can see what causes it
Monitor the temperature of the mix behind the screed from truck exchanges
Excessive differences in mixture temperature should be addressed by evaluating the density in the area in question and adjusting the paving operations accordingly

## Slide 35: Pavement Performance

## Slide 36: Statewide Pavement Performance
Deficient Pavements (%) |  |  |  |  |  |  |  |  |  |  | 
Criteria | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020
Overall | 12.4 | 11.1 | 9.4 | 8.4 | 7.3 | 7.7 | 8.5 | 8.2 | 8.7 | 12.6 | 12.5
Ride | 2.6 | 2.6 | 1.9 | 2.1 | 1.7 | 2.0 | 1.3 | 1.2 | 1.1 | 1.4 | 1.3
Crack | 10.9 | 9.7 | 7.9 | 6.8 | 6.0 | 6.4 | 7.3 | 7.1 | 7.7 | 11.4 | 11.4
Rut | 0.6 | 0.6 | 0.5 | 0.5 | 0.4 | 0.4 | 0.3 | 0.2 | 0.3 | 0.3 | 0.3
Statutory Requirement
  Ensure 80% of pavement on the State Highway System meets Department standards.

## Slide 37: Deficient Pavements by Facility Type
Roadway | Interstate | Arterials | Turnpike
Lane Miles | 8,677 | 33, 937 | 2, 361
Deficient Lane Miles | 699 | 4,758 | 178
% Lane Miles Deficient | 8.1% | 14.0% | 7.5%

## Slide 38: Historical Statewide Performance

## Slide 39: Lane Miles Resurfaced and Deficient Lane Miles

## Slide 40: District 1 Historical Performance

## Slide 41: District 2 Historical Performance

## Slide 42: District 3 Historical Performance

## Slide 43: District 4 Historical Performance

## Slide 44: District 5 Historical Performance

## Slide 45: District 6 Historical Performance

## Slide 46: District 7 Historical Performance

## Slide 47: Turnpike Historical Performance

## Slide 48: Specification Updates

## Slide 49: July 2020 Workbook
Section 334 – Superpave Asphalt Concrete
  The allowable maximum lift thickness of Type SP-12.5 mixtures was increased from 2 ½ inches to 3 inches.

## Slide 50: January 2021 Workbook
Section 234 – Superpave Asphalt Base
  Type SP-19.0 mixes allowed for base
  New allowable layer thicknesses for base courses
    Type B-12.5 & Type SP-12.5: 1 ½ to 3 ½ inches
    Type SP-19.0: 2 to 4 inches
    Density testing required on the first lift of base placed on subgrade if Type SP-19.0 is used or the thickness is 3 ½ inches for Type B-12.5 & Type SP-12.5

## Slide 51: January 2021 Workbook
Section 334 – Superpave Asphalt Concrete
  Updated requirements for continuous RAP stockpiles.
  Increased allowable RAP usage (up to 30%) for structural courses containing PG 76-22 binder. RAP usage above 20% based on RAP properties (percent passing the #16 sieve and high PG grade of the recovered RAP binder).
  Updated requirements for instances where SGC pills are damaged or don’t compare.
  Updated language for binder and mix recovery sampling and testing.

## Slide 52: Proposed changes for July 2021 Workbook
Section 334 – Superpave Asphalt Concrete
  Revised density requirements for unsignalized side streets
  Revised specification limits for density testing
    Increased the density upper specification limit
    Revised density ranges on the small quantity pay table
Section 337 – Asphalt Concrete Friction Courses
  Liquid anti-strip additive required in all FC-5 mixtures
  1.5% hydrated lime required in FC-5 mixtures containing Nova Scotia granite

## Slide 53: Thank You
Questions?