SECTION 720—WATER
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720.2  WATER FOR USE OTHER THAN IN MIXING OR CURING CEMENT CONCRETE, MORTAR, OR GROUT—Suitable clean water may be used without testing. If the water source is relatively shallow, enclose the intake to exclude silt, mud, grass, or other undesirable foreign material.


720.3  WATER FOR ONLY CURING CEMENT CONCRETE, MORTAR, OR GROUT— Use water that is reasonably clean, free from vegetable matter, oil, acid, alkali, sugar, or other substances injurious to the finished product. Water must conform to ASTM C1602, Table 2. Water used for curing will be tested to determine the hydrogen ion concentration of the water, as determined electrometrically or colorimetrically in conjunction with the necessary indicator. Water sources less than pH 4.5 or more than pH 8.5 may not be used for curing.
